LAGOS STATE MATERIALS TESTING LABORATORY

IN-SITU INTEGRITY TEST (NON-DESTRUCTIVE) OF COMPRESSIVE STRENGTH OF STRUCTURAL MEMBERS

| FIELD | VALUE |
| --- | --- |
| Report No | 2099 / MTL/NDR/2027 |
| Project | test gps |
| Client | - |
| Site Address | 12, Godwin Oghoanika Drive Greenland Estate Idowu Egba Bus Stop, ghjk, Lagos |
| Date of Test | 11/09/2026 |

NOTE: this Word document is an editable working copy. The certified document of record is the PDF edition archived (SHA-256 checksummed) on the platform.

1.0 INTRODUCTION

Non-Destructive Test (NDT), as the name implies, means that the material under test is not damaged during test. Direct measurement of the strength of concrete involves destructive stresses and cannot be used for determining the quality of already cast concrete. It is for this reason that direct methods are not employed in determining the strength of in-situ concrete. As a result, indirect method was used.

In compliance with the Mandatory Non-Destructive Test requirement of the Lagos State Government, a Non-Destructive compressive strength test (Structural Integrity Test) was conducted on the project "test gps" located at 12, Godwin Oghoanika Drive Greenland Estate Idowu Egba Bus Stop, ghjk, Lagos. The map showing the exact location of the site is on the Location Map page of this report.

The drawings of the building available on the platform are reproduced in the Appendix of this report. Structural drawing was not provided to the platform; therefore, **assumed strength of 25N/mm2** was used for the analysis of the structural elements.

2.0 PURPOSE OF INVESTIGATION

The purpose of the investigation is to:

Determine the present status of the structures from the outcome of the visual and Non-Destructive test of the tested structures to ascertain their state with respect to BS EN 12504-4:2021, ASTM C597-09.

Determine the ongoing concrete strength of the structure with respect to BS 8110: Part 1 1997.

Provide engineering advice based on the visual and Non-Destructive test conducted.

To comply with government's statutory requirements.

3.0 LITERATURE REVIEW

Ultrasonic Pulse Velocity (UPV) testing is a non-destructive testing technique used for assessing the quality, uniformity, and internal condition of hardened concrete. The method operates by transmitting high-frequency ultrasonic waves through concrete and measuring the travel time between transmitting and receiving transducers.

The pulse velocity is calculated using the relationship:

UPV = L / t

L = Distance between transducers (mm)

t = Pulse transit time (microseconds)

The testing procedure and interpretation of results are conducted in accordance with international standards including ASTM C597 (2020), BS EN 12504-4:2004 and ACI 228.2R (2018).

Estimated compressive strength (E.C.S) values in this report are derived from the project-specific calibration curve established for this project under the Nexucon Link procedure: f_cu = 83.9758 + -0.0206125 x V + 1.43746e-06 x V^2 (f_cu in N/mm2, V the pulse velocity in m/s). Reference: Project calibration (BS 1881-203 / EN 12504-4 basis). The curve was fitted from 5 real calibration pair(s) (cube/core tests against field pulse velocity measurements). The curve is valid over the calibrated velocity range 2106 - 5000 m/s; velocities outside that range are reported without an E.C.S estimate rather than extrapolated. Source: Project calibration regression (5 real UPV + cube pairs). BS 1881-203:1999 notes that no unique velocity-strength relationship exists for all concretes; the curve above is the project-specific calibration applied to every result in Section 5.0.

Derivation of the reported results: each test point velocity is V = L / t; the element pulse velocity is the arithmetic mean of its point velocities, V(element) = (V1 + V2 + ... + Vn) / n; and the estimated compressive strength follows the project-specific calibration above, f_cu = 83.9758 + -0.0206125 x V + 1.43746e-06 x V^2, with V expressed in m/s. Pulse velocities in the Section 5.0 tables are reported in metres per second (m/s); 1 km/s = 1000 m/s.

Worked example (first element tested, Floor:200THK RC SLAB): VA = 120 mm / 30.1 us = 3986.71 m/s; VB = 120 mm / 29.8 us = 4026.85 m/s; VC = 120 mm / 30.3 us = 3960.40 m/s. V(element) = mean of 3 points = 3991.32 m/s (3.991 km/s). f_cu from the project calibration above at V = 3991.32 m/s = 24.60 N/mm2.

4.1 VISUAL TEST

From the visual inspection conducted on the structure the following observations were noted and recorded as at the time of test;

Fghjk observed at lagos, Nigeria on Floor:200THK RC SLAB (see pic i).

Some observations were made at LADON-EXXOL-MOBIL on Floor:200THK RC SLAB (see pic ii).

We notices that the crack depth is about 70mm observed at LADOL-EXXON-MOBIL on Floor:200THK RC SLAB (see pic iii).

Smooth finishing observed at lagos, Nigeria on Floor:200THK RC SLAB.

Some observations were made at LADON-EXXOL-MOBIL on Floor:200THK RC SLAB:780904 (see pic iv).

Smooth, no honeycombing observed at East elevation on Floor:200THK RC SLAB:780904.

We noticed that from the visual inspection, it was observed tha few panels were damping at LADDOL-EXXON-MOBIL on Floor:200THK RC SLAB:780904 (see pic v).

Smooth, no honeycombing observed at East elevation on Floor:200THK RC SLAB:780904.

We noticed that from the visual inspection, it was observed tha few panels were damping at LADDOL-EXXON-MOBIL on Floor:200THK RC SLAB:780904 (see pic vi).

Smooth, no honeycombing observed at East elevation on Floor:200THK RC SLAB:780995.

Nothing observed at test on Floor:200THK RC SLAB:780995 (see pic vii).

Smooth, no honeycombing observed at East elevation on Floor:200THK RC SLAB:780995.

First day observed at lagos state on Floor:200THK RC SLAB:781142 (see pic viii).

4.2 METHODOLOGY

This test is determined by using the Portable Ultrasonic Non-Destructive Digital Indicating Tester (PUNDIT). Non-Destructive, as the name implies, means that the materials being tested are not damaged during the test.

In the Non-Destructive Test, some properties of concrete were measured. These were used to estimate the strength of the concrete, its elastic behavior and durability, hence determining the integrity of the structural member.

CONCRETE

Pulse velocity measurements made on concrete structures are used for quality control purposes. In comparison with mechanical tests on control samples such as cubes or cylinders, pulse velocity measurements have the advantage that they relate directly to the concrete in the structure rather than to samples, which may not be always truly representative of the concrete in situ.

A pulse of longitudinal vibrations is produced by an electro-acoustical transducer, which is held in contact with one surface of the concrete under test. When the pulse generated is transmitted into the concrete from the transducer using a certified coupling gel material, it undergoes multiple reflections at the boundaries of the different material phases within the concrete. A complex system of stress waves develops, which includes both longitudinal and shear waves, and propagates through the concrete. The first waves to reach the receiving transducer are the longitudinal waves, which are converted into an electrical signal by a second transducer. Electronic timing circuits enable the transit time (T) of the pulse to be measured. This test is conducted for assessing the quality and integrity of concrete by passing ultrasound waves through the specimen under test.

The Pundit test equipment can also determine the following:

The homogeneity and uniformity of the concrete.

Changes in the strength of the concrete which may occur with time.

The quality of the concrete in relation to standard requirements.

The quality of one element of concrete in relation to another.

Estimated compressive strength conversion: f_cu = 83.9758 + -0.0206125 x V + 1.43746e-06 x V^2 (f_cu in N/mm2, V in m/s). The full calibration statement is given in Section 3.0.

4.3 REINFORCING BAR (REBAR) ASSESSMENT

No rebar assessment was recorded during this investigation.

4.4 EQUIPMENT

No field device was recorded against these tests.

5.0 ANALYSIS OF TEST RESULT

5.1 CRACK DEPTH MEASUREMENTS (TIME-DIFFERENCE METHOD)

| ELEMENT | POINT | SPACING L (MM) | T CRACKED (US) | T UNCRACKED (US) | CRACK DEPTH (MM) | MEAN DEPTH (MM) / REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB | A | 120.0 | 34.2 | 29.7 | 34.3 |  |
|  | B | 120.0 | 12.0 | 25.0 | - | 34.3 / Depth exceeds 25 mm - structural review required |

| ELEMENT | POINT | SPACING L (MM) | T CRACKED (US) | T UNCRACKED (US) | CRACK DEPTH (MM) | MEAN DEPTH (MM) / REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB | A | 240.0 | 40.0 | 35.0 | 66.4 | 66.4 / Depth exceeds 25 mm - structural review required |

| ELEMENT | POINT | SPACING L (MM) | T CRACKED (US) | T UNCRACKED (US) | CRACK DEPTH (MM) | MEAN DEPTH (MM) / REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| M_Concrete-Rectangular Beam 225 x 600mm | A | 200.0 | 52.1 | 50.1 | 28.5 |  |
|  | B | 200.0 | 53.0 | 50.2 | 33.9 | 31.2 / Depth exceeds 25 mm - structural review required |

| ELEMENT | POINT | SPACING L (MM) | T CRACKED (US) | T UNCRACKED (US) | CRACK DEPTH (MM) | MEAN DEPTH (MM) / REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| M_Concrete-Rectangular Beam 225 x 600mm | A | 200.0 | 52.1 | 50.1 | 28.5 |  |
|  | B | 200.0 | 53.0 | 50.2 | 33.9 | 31.2 / Depth exceeds 25 mm - structural review required |

| ELEMENT | POINT | SPACING L (MM) | T CRACKED (US) | T UNCRACKED (US) | CRACK DEPTH (MM) | MEAN DEPTH (MM) / REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| M_Concrete-Rectangular Beam 225 x 600mm 801629 | A | 200.0 | 52.1 | 50.1 | 28.5 |  |
|  | B | 200.0 | 53.0 | 50.2 | 33.9 | 31.2 / Depth exceeds 25 mm - structural review required |

| ELEMENT | POINT | SPACING L (MM) | T CRACKED (US) | T UNCRACKED (US) | CRACK DEPTH (MM) | MEAN DEPTH (MM) / REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| M_Concrete-Rectangular Beam 225 x 600mm 801629 | A | 200.0 | 52.1 | 50.1 | 28.5 |  |
|  | B | 200.0 | 53.0 | 50.2 | 33.9 | 31.2 / Depth exceeds 25 mm - structural review required |

SUMMARY OF TEST ANALYSIS

| STRUCTURAL MEMBER | NUMBER TESTED | LOCATION | NO OF POINT TAKEN |
| --- | --- | --- | --- |
| Slab | 10 | Ground Floor | 28 |

SUMMARY OF TEST RESULTS

| Structural Element | PATH LENGTH | TRANSIT TIME | PULSE VELOCITY (M/S) | E.C.S | AVERAGE COMPRESSIVE STRENGTH (N/mm2) | REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB | 120 | 30.1 | 3986.71 | 27.8 |  |  |
|  | 120 | 29.8 | 4026.85 | 28.1 | 24.6 | POOR |
|  | 120 | 30.3 | 3960.40 | 27.5 |  |  |

| Structural Element | PATH LENGTH | TRANSIT TIME | PULSE VELOCITY (M/S) | E.C.S | AVERAGE COMPRESSIVE STRENGTH (N/mm2) | REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB | 120 | 30.0 | 4000.00 | 27.9 |  |  |
|  | 120 | 33.3 | 3603.60 | 24.3 | 26.4 | GOOD (POINT SPREAD 396 M/S, ±5.2%) |

| Structural Element | PATH LENGTH | TRANSIT TIME | PULSE VELOCITY (M/S) | E.C.S | AVERAGE COMPRESSIVE STRENGTH (N/mm2) | REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB | 120 | 30.1 | 3986.71 | 27.8 |  |  |
|  | 120 | 29.8 | 4026.85 | 28.1 | 24.6 | POOR |
|  | 120 | 30.3 | 3960.40 | 27.5 |  |  |

| Structural Element | PATH LENGTH | TRANSIT TIME | PULSE VELOCITY (M/S) | E.C.S | AVERAGE COMPRESSIVE STRENGTH (N/mm2) | REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB 780904 | 120 | 30.0 | 4000.00 | 27.9 |  |  |
|  | 120 | 29.7 | 4040.40 | 28.2 | 25.6 | GOOD (POINT SPREAD 437 M/S, ±5.6%) |
|  | 120 | 33.3 | 3603.60 | 24.3 |  |  |

| Structural Element | PATH LENGTH | TRANSIT TIME | PULSE VELOCITY (M/S) | E.C.S | AVERAGE COMPRESSIVE STRENGTH (N/mm2) | REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB 780904 | 120 | 30.1 | 3986.71 | 27.8 |  |  |
|  | 120 | 29.8 | 4026.85 | 28.1 | 24.6 | POOR |
|  | 120 | 30.3 | 3960.40 | 27.5 |  |  |

| Structural Element | PATH LENGTH | TRANSIT TIME | PULSE VELOCITY (M/S) | E.C.S | AVERAGE COMPRESSIVE STRENGTH (N/mm2) | REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB 780904 | 120 | 28.0 | 4285.71 | 30.4 |  |  |
|  | 120 | 30.0 | 4000.00 | 27.9 | 24.1 | POOR (POINT SPREAD 415 M/S, ±5.1%) |
|  | 120 | 31.0 | 3870.97 | 26.7 |  |  |

| Structural Element | PATH LENGTH | TRANSIT TIME | PULSE VELOCITY (M/S) | E.C.S | AVERAGE COMPRESSIVE STRENGTH (N/mm2) | REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB 780904 | 120 | 30.1 | 3986.71 | 27.8 |  |  |
|  | 120 | 29.8 | 4026.85 | 28.1 | 24.6 | POOR |
|  | 120 | 30.3 | 3960.40 | 27.5 |  |  |

| Structural Element | PATH LENGTH | TRANSIT TIME | PULSE VELOCITY (M/S) | E.C.S | AVERAGE COMPRESSIVE STRENGTH (N/mm2) | REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB 780904 | 120 | 30.0 | 4000.00 | 27.9 |  |  |
|  | 120 | 29.0 | 4137.93 | 29.1 | 25.3 | GOOD (POINT SPREAD 534 M/S, ±6.8%) |
|  | 120 | 33.3 | 3603.60 | 24.3 |  |  |

| Structural Element | PATH LENGTH | TRANSIT TIME | PULSE VELOCITY (M/S) | E.C.S | AVERAGE COMPRESSIVE STRENGTH (N/mm2) | REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB 780995 | 45 | 62.5 | 720.00 | - |  |  |
|  | 45 | 67.3 | 668.35 | - | - | NOT ASSESSED (POINT SPREAD 52 M/S, ±3.7%) |

| Structural Element | PATH LENGTH | TRANSIT TIME | PULSE VELOCITY (M/S) | E.C.S | AVERAGE COMPRESSIVE STRENGTH (N/mm2) | REMARK |
| --- | --- | --- | --- | --- | --- | --- |
| Floor 200THK RC SLAB 781142 | 120 | 29.7 | 4040.40 | 28.2 |  |  |
|  | 120 | 30.0 | 4000.00 | 27.9 | 23.6 | POOR (POINT SPREAD 286 M/S, ±3.5%) |
|  | 120 | 28.0 | 4285.71 | 30.4 |  |  |

| STRUCTURAL MEMBER | LOCATION | GOOD (NO, %) | POOR (NO, %) |
| --- | --- | --- | --- |
| Slab | Ground Floor | 3 (30.0%) | 6 (60.0%) |

5.2 SURFACE QUALITY OBSERVATIONS

Floor
200THK RC SLAB A: smooth finishing

Floor
200THK RC SLAB
780904 A: Smooth, no honeycombing

Floor
200THK RC SLAB
780904 B: Minor voids near base

Floor
200THK RC SLAB
780904 A: Smooth, no honeycombing

Floor
200THK RC SLAB
780904 B: Minor voids near base

Floor
200THK RC SLAB
780995 A: Smooth, no honeycombing

Floor
200THK RC SLAB
780995 B: Minor voids near base

Floor
200THK RC SLAB
780995 A: Smooth, no honeycombing

Floor
200THK RC SLAB
780995 B: Minor voids near base

6.0 RECOMMENDATION

Based on the purpose of investigation, the outcome of the Visual and Non-Destructive Test carried out on the building which shows the present state of the building as described in the visual test and depicted in the bar charts, the test analysis revealed that 3 of the 10 structural members tested in the building were good in strength at the time of test, while 6 fell below the statutory 25 N/mm2 strength and require technical advice. It is advised that the client engage a qualified structural engineer and other relevant professionals in the built environment to proffer solution to the defects observed, technical advice on the poor structural members tested and further analyse the structural arrangement to guarantee the stability, integrity and the serviceability of the building.

[URGENT] Structural review of 1 element(s) graded poor or very poor by pulse velocity.

[HIGH] Map and monitor 6 element(s) with crack depth above 25 mm; engage a structural engineer.

[URGENT] Immediate structural engineering review — pulse velocity indicates compromised concrete.

[HIGH] Map crack extent and monitor; engage structural engineer for crack-depth exceedance.

7.0 CONCLUSION

The visual and structural integrity test was conducted in accordance with BS 1881: Part 201: 1986, BS EN 12504-4:2004, BS EN 12504-4:2021.

The Non-Destructive Test analysis as shown in the summary of test result (Section 5.0) shows the percentage of strength for the structural elements tested in the building: 3 of 10 elements (30.0%) attained the assumed 25 N/mm2 strength at the time of test, while 6 elements (60.0%) fell below it.

However, it is imperative to state clearly that non-adherence to the recommendation excludes the testing laboratory of any responsibility.

However, it is imperative to state clearly that non-adherence to the recommendation excludes the testing laboratory of any responsibility.

The test assumed 25 N/mm2 as the strength of the structural members, however a substructure probe is required to ascertain the integrity of the building foundation.

| TESTED BY | APPROVED BY |
| --- | --- |
| ENGR. F. BALOGUN (NDE SPECIALIST) | ADMIN USER |

REPORT INTEGRITY

Content digest (SHA-256 of the underlying test identifiers, results and reading rows):

8b8aecccc26bf25daeb21c1eafd9f834a3320d69030584e246677cec7ae97af6

Generated 11/09/2026 22:11 by Admin User.